Table 1

Chemical content and thermal treatment regimes for binary alloys

| Alloy | Content of elements, atomic per cent |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe | Cr | Cu | Mn | Mo | Ni | V | W | T0C |
| FeW | Basic | 0.17 | 0.22 | 0.14 | 0 | 0.12 | 0 | 0.83 | 750 |
| FeMo | Basic | 0.16 | 0.21 | 0.12 | 0.82 | 0.10 | 0 | 0.02 | 750 |
| FeCr | Basic | 8.67 | 0.20 | 0.23 | 0.10 | 0.09 | 0 | 0.02 | 750 |
| All samples were treated by cold deformation and annealed during 30 hours |  |  |  |  |  |  |  |  |  |

Table 2

Chemical content of ternary alloys

| Alloy | Fe | Cr | Cu | Mn | Mo | Ni | V | W |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FeCrMo | Basic | 8.50 | 0.20 | 0.19 | 0.88 | 0.12 | 0 | 0.02 |
| FeCrV | Basic | 8.40 | 0.12 | 0 | 0 | 0.60 | 4.51 | 0 |
| FeCrW | Basic | 8.72 | 0.21 | 0.21 | 0 | 0.10 | 0 | 0.87 |

Table 3

Results of experiments

| Sample under investigation | τ1/ps | I1/ % | τ2/ ps | I2/ % | χ2 | Third component |
| --- | --- | --- | --- | --- | --- | --- |
| FeCr | 123±2 | 76±2 | 280±30 | 24±5 | 1.1±0.1 | Absent |
| FeMo | 122±2 | 72±2 | 260±20 | 27±6 | 0.9±0.1 | Absent |
| FeW | 118±2 | 70±2 | 250±20 | 30±4 | 1.06±0.10 | Absent |

Table 4

Results of fitting with fixed parameters.

| Material of the sample | τ1/ ps | I1/ % | τ2/ps | I2/ % | τ3/ps | I3/ % | χ2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| FeCr | 115 | 61.8±0.3 | 190 | 27.2±0.5 | 350 | 10.4±0.2 | 1.08±0.04 |
| FeMo | 115 | 60.0±0.3 | 190 | 30.0±0.8 | 350 | 10.1±0.2 | 0.99±0.04 |
| FeW | 115 | 62.1±0.3 | 190 | 26.7±0.8 | 350 | 11.1±0.2 | 1.05±0.04 |

Table 5

Results of ternary alloys investigation experiments (without fixing the decay exponents)

| Material of the sample | τ1/ ps | I1/ % | τ2/ps | I2/ % | τ3/ ps | I3/ % |
| --- | --- | --- | --- | --- | --- | --- |
| FeCrMo | 129±1 | 82.5±0.6 | 316±6 | 18.0±0.6 | 1.08±0.05 | Absent |
| FeCrV | 128±1 | 81.7±0.4 | 314±4 | 18.3±0.6 | 1.10±0.05 | Absent |
| FeCrW | 129±1 | 81.8±0.6 | 317±4 | 18.2±0.6 | 1.03±0.04 | Absent |

Table 6

Results of ternary alloys investigation experiments (with fixing the decay exponents)

| Material of the sample | τ1/ ps | I1/ % | τ2/ ps | I2/ % | τ3/ps | I3/ % | χ2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| FeCrMo | 115 | 60.4.±0.4 | 190 | 30±1 | 350 | 9.5±0.4 | 1.07±0.09 |
| FeCrV | 115 | 61.1±0.6 | 190 | 28±1 | 350 | 10.4±0.5 | 1.12±0.09 |
| FeCrW | 115 | 60.3±04 | 190 | 30±1 | 350 | 9.7±0.4 | 1.002±0.098 |

Table 7

Results of calculations. Relative error is 1%

| Material of the sample | μ12/ 108 с-1 | μ13/ 108 с-1. | С2/ 1015сm-3 | С3/1015сm-3 |
| --- | --- | --- | --- | --- |
| FeCr | 9,33 | 6.07 | 2.58 | 1.53 |
| FeMo | 10.3 | 5.89 | 2.85 | 1.48 |
| FeW | 9.16 | 6.49 | 2.54 | 1.64 |

Table 8

The calculated results for ternary alloys. The relative error of the measurements is 4%

| Material of the sample | μ12/ 108 с-1 | μ13/ 108 с-1. | С2/1015сm-3 | С3/ 1014сm-3 |
| --- | --- | --- | --- | --- |
| FeCrMo | 10.3 | 5.55 | 2.85 | 1.40 |
| FeCrV | 9.6 | 6.07 | 2.66 | 1.53 |
| FeCrW | 10.3 | 5.56 | 2.85 | 1.41 |