Table 1 TG: H2 reduction, non-isothermal experimental conditions

| Number | Sample | Final temperature (°C) | Heating rate (°C∙min-1) | Flow of H2 (mL∙min-1) |
| --- | --- | --- | --- | --- |
| 1-1 | NiO | 700 | 10 | 40 |
| 1-2 | NiO | 700 | 15 | 40 |
| 1-3 | NiO | 700 | 20 | 40 |
| 2-1 | NiFe2O4 | 1000 | 10 | 40 |
| 2-2 | NiFe2O4 | 1000 | 15 | 40 |
| 2-3 | NiFe2O4 | 1000 | 20 | 40 |
| 3-1 | Fe2O3 | 1000 | 10 | 40 |
| 3-2 | Fe2O3 | 1000 | 20 | 40 |
| 4-1 | Fe2O3 + NiO | 1000 | 10 | 40 |
| 4-2 | Fe2O3 + NiO | 1000 | 15 | 40 |
| 4-3 | Fe2O3 + NiO | 1000 | 20 | 40 |
| 5-1 | Fe2O3 + Ni | 1000 | 10 | 40 |

Table 2 TG: C reduction, non-isothermal experimental conditions

| Number | Sample | Mass ratio (wt%) | Mass of sample (mg) | Final temperature (°C) |
| --- | --- | --- | --- | --- |
| 1 | C + NiO | 30.2:69.8 | 15.030 | 900 |
| 2 | C + Fe2O3 | 30.0:70.0 | 15.000 | 1100 |
| 3 | C + NiO + Fe2O3 | 30.1:22.3:47.6 | 15.020 | 1000 |
| 4 | C + NiFe2O4 | 30.1:69.9 | 15.040 | 1100 |
| 5 | C + Ni + Fe2O3 | 30.0:18.8:51.2 | 15.000 | 1100 |
| 3-a | C + NiO + Fe2O3 | 30.1:22.3:47.6 | 15.010 | 750 |
| 4-a | C + NiFe2O4 | 30.1:69.9 | 15.020 | 895 |
| 4-b | C + NiFe2O4 | 30.1:69.9 | 15.010 | 938 |
| 5-a | C + Ni + Fe2O3 | 30.0:18.8:51.2 | 15.020 | 890 |

Table 3 Isothermal experimental conditions in the resistance furnace

| Number | Sample | Reduction temperature (°C) | Reduction time (min) |
| --- | --- | --- | --- |
| 1-1 | NiFe2O4 | 450 | 20 |
| 1-2 | NiFe2O4 | 500 | 20 |
| 1-3 | NiFe2O4 | 550 | 20 |
| 1-4 | NiFe2O4 | 600 | 20 |
| 1-5 | NiFe2O4 | 650 | 20 |
| 1-6 | NiFe2O4 | 700 | 20 |

Table 4 Suggested mathematical modeling of reaction kinetics

| Symbol | Mechanism | The integral form of reaction mechanism |
| --- | --- | --- |
| D1 | 1D internal diffusion |  |
| D2 | 2D internal diffusion |  |
| D3 | 3D internal diffusion |  |
| D4 | 3D internal diffusion(Ginstling–Brounshtein equation) |  |
| A1 | 1D formation and growth of nuclei |  |
| A2 | 2D formation and growth of nuclei |  |
| A3 | 3D formation and growth of nuclei |  |
| A4 | 4D formation and growth of nuclei |  |
| R1 | 2D phase-boundary-controlled reaction |  |
| R2 | 3D phase-boundary-controlled reaction |  |
| P1 | Power law |  |
| P2 | Power law |  |
| P3 | Power law |  |
| P4 | Power law |  |
| Au | Autocatalytic reaction |  |

Table 5 Reduction characteristics of the five oxide systems using H2 as reductant

| Oxide | Stage I (°C) | Stage II (°C) | Reduction degree (%) | Maximum reaction rate (%∙min-1) | Temp. at maximum rate (°C) | Average rate (%∙min-1) |
| --- | --- | --- | --- | --- | --- | --- |
| NiO | 302–602 |  | 100 | 8.6 | 329 | 3.3 |
| Fe2O3 | 373–404 | 404–520 | 100 | 11.5 | 504 | 6.7 |
| NiFe2O4 | 323–350 | 350–513 | 100 | 11.4 | 478 | 5.3 |
| Fe2O3+NiO | 291–364 | 364–504 | 100 | 9.7 | 461 | 4.8 |
| Fe2O3 + Ni | 336–490 |  | 100 | 13.6 | 470 | 6.7 |

Table 6 Reduction characteristics of the five oxide systems using C as reductant

| Oxide | Stage I (°C) | Stage II (°C) | Stage III (°C) | α (%) | Maximum reaction rate (%∙min-1) | Temp. at maximum rate (°C) | Average rate (%∙min-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| NiO | 771–783 |  |  | 89.2 | 75.7 | 778 | 74.3 |
| Fe2O3 | 702–878 | 878–969 | 969–1017 | 100 | 47.2 | 991 | 3.2 |
| NiFe2O4 | 757–895 | 895–938 | 938–1000 | 92.1 | 8.0 | 979 | 4.5 |
| Fe2O3 + NiO | 745–895 | 895–910 |  | 99.2 | 57.9 | 923 | 6.1 |
| Fe2O3 + Ni | 681–890 | 890–963 | 963–1010 | 100 | 30.0 | 991 | 3.0 |

Table 7 Reduction products for NiFe2O4

| H2 reduction |  |  | C reduction |  |  |
| --- | --- | --- | --- | --- | --- |
| Reduction temperature (°C) | Reduction products | Reduction degree (%) | Reduction temperature (°C) | Reduction products | Reduction degree (%) |
| 450 | Fe2O3, NiO, Fe3O4 | 1.1 | 895 | Fe3O4, Ni | 18.6 |
| 500 | Fe3O4, Ni, (Fe, Ni) | 60.4 | 938 | (Fe, Ni), FeNi3, FeO | 48.8 |
| 550 | Fe3O4, Ni, (Fe, Ni), Fe0.64Ni0.36, Fe | 63.3 | 1100 | (Fe, Ni), FeNi3, Fe5C2 | 92.1 |
| 600 | Fe3O4, Ni, (Fe, Ni), Fe0.64Ni0.36, Fe | 88.6 |  |  |  |
| 700 | Fe0.64Ni0.36, Fe | 96.8 |  |  |  |

Table 8 Reaction parameters and mechanisms of oxide reduction with H2

| Process | Temperature range (°C) | Activation energy (kJ∙min-1) | Published activation energy (kJ∙min-1) | Mechanism |
| --- | --- | --- | --- | --- |
| NiO → Ni | 280–657 | 87.8 | 90.8 [4] | phase-boundary reaction. |
| Fe2O3 → Fe3O4 Fe3O4 → Fe | 340–430 430–592 | 185.1 53.8 | 107 [13] 54 [14] | phase-boundary reaction 4D formation and growth of nuclei |
| NiFe2O4 → Fe/Ni | 320–632 | 69.4 | 62.6 [11] | autocatalytic reaction |
| Fe2O3 + NiO → Fe/Ni | 280–415 415–600 | 71.3 |  | phase-boundary reaction and autocatalytic reaction |