Table 1 Suggested mathematical modeling of reaction kinetics

| Symbol | Mechanism | The integral form of reaction mechanism |
| --- | --- | --- |
| D1 | 1D internal diffusion |  |
| D2 | 2D internal diffusion |  |
| D3 | 3D internal diffusion |  |
| D4 | 3D internal diffusion(Ginstling–Brounshtein equation) |  |
| A1 | 1D formation and growth of nuclei |  |
| A2 | 2D formation and growth of nuclei |  |
| A3 | 3D formation and growth of nuclei |  |
| A4 | 4D formation and growth of nuclei |  |
| R1 | 2D phase-boundary-controlled reaction |  |
| R2 | 3D phase-boundary-controlled reaction |  |
| P1 | Power law |  |
| P2 | Power law |  |
| P3 | Power law |  |
| P4 | Power law |  |
| Au | Autocatalytic reaction |  |

Table 2 Reaction parameters and mechanisms of oxide reduction with H2

| Process | Temperature range (°C) | Activation energy (kJ∙min-1) | Published activation energy (kJ∙min-1) | Mechanism |
| --- | --- | --- | --- | --- |
| NiO → Ni | 280–657 | 87.8 | 90.8 [4] | phase-boundary reaction. |
| Fe2O3 → Fe3O4 Fe3O4 → Fe | 340–430 430–592 | 185.1 53.8 | 107 [13] 54 [14] | phase-boundary reaction 4D formation and growth of nuclei |
| NiFe2O4 → Fe/Ni | 320–632 | 69.4 | 62.6 [11] | autocatalytic reaction |
| Fe2O3 + NiO → Fe/Ni | 280–415 415–600 | 71.3 |  | phase-boundary reaction and autocatalytic reaction |