Table 1 non-isothermal experimental conditions

| Run No. | Sample | Mass of sample (mg) | Heating rate (°C∙min-1) | Final temperature (°C) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| CA-1 | C + NiO | 15.030 | 10 | 900 |  |
| CA-2 | C + Fe2O3 | 15.000 | 10 | 1100 |  |
| CA-3 | C + NiO + Fe2O3 | 15.020 | 10 | 1000 |  |
| CA-4 | C + NiFe2O4 | 15.040 | 10 | 1100 |  |
| CA-5 | C + Ni + Fe2O3 | 15.000 | 10 | 1100 |  |
| CB-1 | C + NiO + Fe2O3 | 15.010 | 10 | 750 |  |
| CB-1 | C + NiFe2O4 | 15.020 | 10 | 895 |  |
| CB-1 | C + NiFe2O4 | 15.010 | 10 | 938 |  |
| CB-1 | C + Ni + Fe2O3 | 15.020 | 10 | 890 |  |
| HA-1 | NiO | 30.3 | 10 | 700 |  |
| HA-2 | NiO | 30.3 | 15 | 700 |  |
| HA-3 | NiO | 30.0 | 20 | 700 |  |
| HA-4 | NiFe2O4 | 30.4 | 10 | 1000 |  |
| HA-5 | NiFe2O4 | 30.1 | 15 | 1000 |  |
| HA-6 | NiFe2O4 | 30.4 | 20 | 1000 |  |
| HA-7 | Fe2O3 | 30.4 | 10 | 1000 |  |
| HA-8 | Fe2O3 | 30.3 | 20 | 1000 |  |
| HA-9 | Fe2O3 + NiO | 30.0 | 10 | 1000 |  |
| HA-10 | Fe2O3 + NiO | 30.0 | 15 | 1000 |  |
| HA-11 | Fe2O3 + NiO | 30.1 | 20 | 1000 |  |
| HA-12 | Fe2O3 + Ni | 30.3 | 10 | 1000 |  |

Table 2 Isothermal experimental conditions

| Run No. | Sample | Mass of sample (g) | Reduction temperature (°C) | Reduction time (min) |
| --- | --- | --- | --- | --- |
| HB-1 | NiFe2O4 | 3.004 | 450 | 20 |
| HB-2 | NiFe2O4 | 3.001 | 500 | 20 |
| HB-3 | NiFe2O4 | 3.002 | 550 | 20 |
| HB-4 | NiFe2O4 | 3.002 | 600 | 20 |
| HB-5 | NiFe2O4 | 3.000 | 650 | 20 |
| HB-6 | NiFe2O4 | 2.999 | 700 | 20 |

Table 3 Reaction parameters and mechanisms of oxide reduction with H2

| Process | Activation energy (kJ∙min-1) | Published activation energy (kJ∙min-1) | The integral form of reaction mechanism | Mechanism |
| --- | --- | --- | --- | --- |
| NiO → Ni | 87.8 | 90.8 [4] |  | phase-boundary reaction. |
| Fe2O3 → Fe3O4 Fe3O4 → Fe | 185.1 53.8 | 107 [13] 54 [14] |  | phase-boundary reaction 4D formation and growth of nuclei |
| NiFe2O4 → Fe/Ni | 69.4 | 62.6 [11] |  | autocatalytic reaction |
| Fe2O3 + NiO → Fe/Ni | 71.3 |  |  | phase-boundary reaction and autocatalytic reaction |