Thanks for your and the reviewers’ suggestion!

I confirm that my manuscript can be accepted for publication in the Journal of Mining and Metallurgy, Section B: Metallurgy.

For the comments:

- Experimental conditions

  - The thermocouple in thermal analyzer are divided into two types: one is directly bared in the reaction space without any protection. The material of thermocouple decides that it can not contact with reducing atmosphere. The thermal analyzer for reduction with C belongs to this type. It can not be used for reduction with H2; And the other is protected, such as the one for reduction with H2.

  - The sample mass can be seen from Table 1 and 2.

  - Ceramic crucibles, which were outfitted with the thermal analyzers, were used in non-isothermal experiments. And alumina crucibles were used in isothermal experiments.

  - The flow of H2 is 40ml/min for reduction with H2.

  - The molar ratio of elements of Fe and Ni in these complex sample is always 2:1, and in the reduction experiments with C, the C content is 30%.

Sample preparation: (1)weigh;(2)mix.

  - Taking Ar as protective atmosphere, its flow is 30ml/min for reduction with C.

  - The heating rates for non-isothermal experiments and the reaction times can be seen from Table 1 and 2, respectively.

  - The purities of Ni, NiO, Fe2O3 and activated carbon are AR.

  - The values of heating rates in experiments are in the range of normal heating rate of the instruments. Therefore, there is no influence of the heating rate on reduction temperatures.

Table 1 non-isothermal experimental conditions

| Run No. | Sample | Mass of sample (mg) | Heating rate (°C∙min-1) |  |
| --- | --- | --- | --- | --- |
| CA-1 | C + NiO | 15.030 | 10 |
| CA-2 | C + Fe2O3 | 15.000 | 10 |
| CA-3 | C + NiO + Fe2O3 | 15.020 | 10 |
| CA-4 | C + NiFe2O4 | 15.040 | 10 |
| CA-5 | C + Ni + Fe2O3 | 15.000 | 10 |
| CB-1 | C + NiO + Fe2O3 | 15.010 | 10 |
| CB-1 | C + NiFe2O4 | 15.020 | 10 |
| CB-1 | C + NiFe2O4 | 15.010 | 10 |
| CB-1 | C + Ni + Fe2O3 | 15.020 | 10 |
| HA-1 | NiO | 30.3 | 10 |
| HA-2 | NiO | 30.3 | 15 |
| HA-3 | NiO | 30.0 | 20 |
| HA-4 | NiFe2O4 | 30.4 | 10 |
| HA-5 | NiFe2O4 | 30.1 | 15 |
| HA-6 | NiFe2O4 | 30.4 | 20 |
| HA-7 | Fe2O3 | 30.4 | 10 |
| HA-8 | Fe2O3 | 30.3 | 20 |
| HA-9 | Fe2O3 + NiO | 30.0 | 10 |
| HA-10 | Fe2O3 + NiO | 30.0 | 15 |
| HA-11 | Fe2O3 + NiO | 30.1 | 20 |
| HA-12 | Fe2O3 + Ni | 30.3 | 10 |

Table 2 Isothermal experimental conditions

| Run No. | Sample | Mass of sample (g) | Reduction temperature (°C) | Reduction time (min) |
| --- | --- | --- | --- | --- |
| HB-1 | NiFe2O4 | 3.004 | 450 | 20 |
| HB-2 | NiFe2O4 | 3.001 | 500 | 20 |
| HB-3 | NiFe2O4 | 3.002 | 550 | 20 |
| HB-4 | NiFe2O4 | 3.002 | 600 | 20 |
| HB-5 | NiFe2O4 | 3.000 | 650 | 20 |
| HB-6 | NiFe2O4 | 2.999 | 700 | 20 |

- I’ll accept this suggestion.

- I’ll accept this suggestion.

- I’ll accept this suggestion.

For the comments, the corresponding modification have done in the text.

Thank you for your attention!

Best wishes!

Wei.