Table I. Main elements in EGM gold mine tailings, determined by X-ray fluorescence analysis

| Elements | SiO2 | Fe2O3 | SO3 | Al2O3 | K2O | ZnO | CaO | P2O5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Weight % | 37.49 | 34.26 | 21.13 | 4.20 | 1.47 | 0.90 | 0.35 | 0.20 |

Table II. Minor elements in EGM gold mine tailings, determined by scanning electron microscopy coupled with energy-dispersive X‐ray spectrometry

| Elements | Fe | O | Si | S | Al | K | Mg |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Weight % | 41.06 | 32.64 | 15.34 | 7.11 | 1.94 | 0.82 | 0.33 |

Table III. Minor elements in the gold mine tailings after desulphurization roasting, determined by scanning electron microscopy coupled with energy-dispersive X‐ray spectrometry

| Elements | Fe | O | Si | S | Al | K | Mg |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Weight % | 52.57 | 27.26 | 14.73 | 0.36 | 1.57 | 0.94 | 0.33 |

Table IV. Gibbs free-energy changes in the chemical reactions between the major oxides in the gold mine tailings

| Temperature,°С | CuO | 3CaO·P2O5 | CaO·SiO2 | 2FeO·SiO2 | 2CaO·Al2O3 | CaO·FeO·SiO2 | CaO·Al2O3 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 700 | -137.00 | -694.706 | -90.856 | -23.303 | -13.015 | -14.92 | -14.12 |
| 800 | -120.24 | -688.638 | -90.898 | -21.952 | -13.191 | 5.857 | -12.315 |
| 900 | -103.64 | -682.602 | -90.802 | -20.442 | -13.423 | 28.5 | -9.979 |
| 1000 | -87.187 | -676.714 | -90.732 | -18.954 | -13.717 | 52.722 | -7.142 |
| 1100 | -70.552 | -671.069 | -90.702 | -17.522 | -14.076 | 78.403 | -3.827 |
| 1200 | -52.382 | -666.395 | -90.715 | -16.17 | -14.503 | 105.449 | -0.058 |
| 1300 | -39.145 | -662.62 | -90.774 | -14.925 | -15.001 | 133.777 | 4.147 |
| 1400 | -27.876 | -659.046 | -90.882 | -13.134 | -15.569 | 163.654 | 8.769 |
| 1500 | -16.812 | -655.652 | -91.04 | -9.233 | -16.211 | 195.814 | 13.793 |
| 1600 | -5.939 | -652.416 | -91.249 | -5.483 | -16.925 | 229.081 | 19.204 |