Figures Extracted

Figure 1. Quinary system Cu-Fe-S-O-SiO2, T and P fixes

Figure 2. FeO-Fe2O3-SiO2 ternary system.

Figure 3. Isotherm at 1300 °C and isobars of oxygen potentials for ternary systems

FeO–Fe2O3–SiO2 and FeO–Fe2O3–CaO.

Figure 4. Stability diagrams of quaternary system Cu–Fe–O–SiO2: stability areas at 1200°C.

Figure 5. Stability diagram for copper and molybdenum in Cu-Mo-Fe system, 1300ºC.

(a)	(b)

Figure 6. SEM analysis for molybdenum (a) and iron (b) distribution in slag.

Phase 3

% Cu =0.1824

% Fe = 11.28

% Si = 31.76

% S = 0.2495

% Mo= 0.1034

% 2FeO·SiO2= 20.57

% SiO2= 67.95

Phase 2:

% Cu = 0.037

% Fe = 63.37

% Si = 0.394

% S = 0

% Mo= 1.245

% 2FeO∙SiO2= 2.85

% SiO2= 0.84

Phase 4

% Cu = 0.027

% Fe = 52.03

% Si = 7.12

% S = 0

% Mo= 4.36

% 2FeO∙SiO2=51.67

% SiO2=1 5.23

Phase 1

% Cu =0.032

% Fe = 52.17

% Si= 3.08

% S = 0

% Mo= 6.35

% 2FeO·SiO2=22.35 % SiO2=6.59

Figure 7. SEM characterization of a copper slag.

Figure 8. Extraction of molybdenum related to magnetite content.

Figure 9. Concentration of copper and iron as function of time.

Figure 10. Slag and iron-rich alloy obtained at 1460ºC in an alumina crucible.

Figure 11. Flowsheet proposed for metal/material extraction from non ferrous slags

.

Tables Extracted

Table 1. Estimates of Global Smelter Slag Tonnage

| Smelter Type | Metal via Smelter kt | Recovery Factor % | Smelter Metal Input kt | Smelter Feed Grade % | Smelter Input kt | Factor Slag/Feed Wt Ratio | Slag Tonnage kt |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Copper | 12,000 | 95 | 12,600 | 27 | 47,000 | 0.8 | 37,000 |
| Nickel | 450 | 95 | 470 | 10 | 4,700 | 1 | 4,700 |
| Fe-Ni | 300 | 95 | 320 | 2 | 16,000 | 1 | 16,000 |
| PGM | 0.3 | 85 | 0.35 | 0.015 | 2,300 | 1 | 2,300 |
| Iron1 | 860,000 | - | - | - | 860,000 | 0.3 | 260,000 |
| Steel1 | 860,000 | - | - | - | 860,000 | 0.2 | 170,000 |
| Cement |  |  |  |  |  |  | 2,700,000 |

1 Metal Output

Table 2. Smelting Industry Product Value and Slag Cleaning Targets

| Industrial Sector | Metal Prod’n kt/y | Price $/t Metal | Metal Revenue Million $/y | Slag kt/y | Slag Cleaning Targets |
| --- | --- | --- | --- | --- | --- |
| Copper | 12,000 | 10,000 | 120,000 | 37,000 | Cu & Au |
| Nickel | 450 | 20,000 | 9,000 | 4,700 | Ni & Co |
| Ferro-nickel | 300 | 20,000 | 6,000 | 16,000 | - |
| PGM | 0.3 | 50,000,000 | 15,000 | 2,300 | Ni-Cu PGM,Cr |
| Blast Fce Iron | 860,000 | 500 | 430,000 | 260,000 | - |
| Steel (via pig) 1 | 860,000 | 200 added | 172,000 | 170,000 | - |
| Notes: |  |  |  |  |  |
| Steel1(Total) | 1,100,000 | 700 | 770,000 | - | - |
| Cement | 2,700,000 | 100 | 270,000 | 2,700,000 | - |

1Includes scrap recycling and DRI