Supplementary Data for

Comparison of the mineralogy and microstructure of EAF stainless steel slags with reference to the cooling path

*Mojca Loncnar, Ana Mladenovič, Marija Zupančič, and Peter Bukovec

Table S1. Chemical composition of sampled EAF S slags. Results for the characterization of EAF S slags (samples Sa, Sw, E3041, E3042, E31, E32, EM1 and EM2) are taken from article Loncnar M., Zupančič M., Bukovec P., Jaklič A., 2009. The effect of water cooling on the leaching behaviour of EAF slag from stainless steel production. Mater. Tech. 43, 315– 321).

|  | CaO | SiO2 | Cr2O3 | MgO | Fe | Al2O3 | MnO |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | w/% |  |  |  |  |
| Sa | 37.5±0.1 | 20.24±0.06 | 12.0±0.1 | 8.690±0.002 | 6.7±0.2 | 6.59±0.06 | 3.54±0.04 |
| Sw | 35.4±0.4 | 19.5±0.2 | 12.7±0.3 | 9.10±0.04 | 7.3±0.5 | 6.65±0.04 | 3.63±0.02 |
| SaT | 35.4±0.1 | 19.4±0.1 | 11.93±0.03 | 8.28±0.01 | 8.0±0.2 | 6.22±0.01 | 3.55±0.01 |
| SwT | 35.74±0.02 | 19.34±0.04 | 11.5±0.2 | 8.79±0.01 | 7.1±0.4 | 6.38±0.02 | 3.55±0.03 |
| E3041 | 41.425±0.002 | 18.82±0.04 | 9.18±0.04 | 9.55±0.04 | 4.4±0.1 | 8.856±0.001 | 3.03±0.01 |
| E3042 | 38.2±0.2 | 18.52±0.05 | 10.61±0.01 | 9.59±0.02 | 5.2±0.1 | 8.08±0.03 | 3.60±0.01 |
| E31 | 36.4±0.1 | 22.4±0.2 | 5.91±0.06 | 13.8±0.1 | 8.0±0.2 | 7.47±0.09 | 3.29±0.01 |
| E32 | 37.34±0.01 | 22.95±0.02 | 5.24±0.06 | 13.6±0.1 | 6.0±0.2 | 7.845±0.004 | 3.23±0.01 |
| EM1 | 43.6±0.1 | 10.78±0.03 | 1.540±0.002 | 10.73±0.04 | 10.g±0.2 | 15.55±0.07 | 1.45±0.03 |
| EM2 | 35.4±0.2 | 18.83±0.04 | 3.04±0.03 | 8.70±0.03 | 10.5±0.1 | 11.13±0.08 | 1.76±0.01 |
| CSa | 43.8±0.4 | 21.3±0.3 | 4.6±0.1 | 10.1±0.1 | 4.9±0.4 | 7.10±0.02 | 1.61±0.01 |
| CSw1 | 40.3±0.1 | 18.9±0.1 | 6.1±0.1 | 9.26±0.01 | 8.1±0.1 | 7.3±0.1 | 1.82±0.01 |
| CSw2 | 40.1±0.7 | 19.7±0.3 | 5.7±0.2 | 9.1±0.1 | 9.3±0.9 | 6.6±0.1 | 1.60±0.01 |
| SSa | 35±0.1 | 19.94±0.03 | 15.2±0.1 | 8.18±0.01 | 6.5±0.3 | 4.33±0.01 | 3.56±0.01 |
| SSw1 | 34.5±0.2 | 19.5±0.1 | 16.4±0.2 | 7.39±0.06 | 6.4±0.1 | 3.73±0.01 | 3.67±0.01 |
| SSw2 | 35.6±0.1 | 18.91±0.02 | 14.38±0.03 | 7.96±0.02 | 6.7±0.1 | 4.40±0.02 | 3.45±0.01 |
| SSSa | 39.7±0.2 | 20.20±0.04 | 12.04±0.04 | 8.15±0.05 | 4.06±0.02 | 6.21±0.03 | 4.31±0.01 |
| SSSw1I | 38.7±0.1 | 20.4±0.1 | 12.2±0.1 | 8.1±0.1 | 4.3±0.1 | 6.01±0.01 | 4.34±0.01 |
| SSSw1II | 38.2±0.1 | 20.7±0.2 | 12.0±0.1 | 9.19±0.02 | 3.47±0.01 | 6.40±0.03 | 4.66±0.03 |
| SSSw2I | 39.21±0.01 | 20.4±0.1 | 12.90±0.02 | 7.75±0.02 | 3.74±0.01 | 5.86±0.03 | 4.57±0.02 |
| SSSw2II | 37.14±0.01 | 22.83±0.02 | 12.15±0.04 | 8.09±0.01 | 3.12±0.03 | 5.12±0.02 | 5.32±0.01 |

Cooling mode: a = air cooling; w1 = immersion; w2 = quenching

|  | F– | TiO2 | V2O5 | Ni | C | S | TOC |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | w/% |  |  |  |  |
| Sa | 0.64±0.01 | 0.99±0.01 | 0.283±0.001 | 0.71±0.06 | 0.16±0.01 | 0.166±0.003 | <0.2 |
| Sw | 0.50±0.01 | 1.03±0.02 | 0.285±0.003 | 0.65±0.09 | 0.23±0.01 | 0.150±0.001 | <0.2 |
| SaT | n.a. | 0.99±0.01 | 0.273±0.001 | 0.59±0.02 | 0.22±0.01 | 0.140±0.001 | <0.2 |
| SwT | n.a. | 1.02±0.01 | 0.275±0.002 | 0.37±0.04 | 0.26±0.01 | 0.140±0.001 | <0.2 |
| E3041 | 1.19±0.02 | 1.01±0.01 | 0.243±0.005 | 0.30±0.03 | 0.17±0.01 | 0.296±0.003 | n.a. |
| E3042 | 0.81±0.01 | 0.842±0.001 | 0.266±0.006 | 0.43±0.04 | 0.18±0.01 | 0.256±0.004 | n.a. |
| E31 | 0.122±0.005 | 0.78±0.01 | 0.139±0.001 | 0.76±0.09 | 0.15±0.01 | 0.095±0.001 | n.a. |
| E32 | 0.129±0.002 | 0.755±0.003 | 0.137±0.002 | 0.76±0.06 | 0.21±0.01 | 0.112±0.003 | n.a. |
| EM1 | 0.83±0.01 | 0.327±0.003 | 0.042±0.001 | 0.11±0.01 | 0.13±0.01 | 0.593±0.005 | n.a. |
| EM2 | 0.84±0.02 | 0.473±0.004 | 0.074±0.001 | 0.18±0.03 | 0.37±0.01 | 0.417±0.003 | n.a. |
| CSa | 0.51±0.01 | 1.22±0.01 | 0.257±0.002 | 0.39±0.03 | 0.065±0.005 | 0.134±0.001 | n.a. |
| CSw1 | 0.53±0.01 | 1.137±0.002 | 0.243±0.001 | 0.60±0.01 | 0.150±0.001 | 0.165±0.001 | n.a. |
| CSw2 | 0.44±0.01 | 1.13±0.01 | 0.255±0.003 | 0.72±0.06 | 0.125±0.005 | 0.126±0.001 | n.a. |
| SSa | 0.45±0.02 | 1.060±0.01 | 0.395±0.001 | 0.46±0.02 | 0.025±0.001 | 0.140±0.001 | n.a. |
| SSw1 | 0.52±0.02 | 1.09±0.01 | 0.377±0.003 | 0.502±0.002 | 0.077±0.001 | 0.140±0.001 | n.a. |
| SSw2 | 0.734±0.001 | 1.12±0.01 | 0.369±0.008 | 0.48±0.01 | 0.086±0.001 | 0.190±0.001 | n.a. |
| SSSa | 0.830±0.001 | 0.984±0.004 | 0.345±0.03 | 0.37±0.06 | 0.065±0.01 | 0.182±0.006 | <0.2 |
| SSSw1I | 0.760±0.001 | 1.02±0.01 | 0.352±0.001 | 0.43±0.02 | 0.115±0.005 | 0.190±0.002 | <0.2 |
| SSSw1II | 0.595±0.005 | 1.14±0.01 | 0.362±0.002 | 0.36±0.05 | 0.110±0.001 | 0.190±0.003 | <0.2 |
| SSSw2I | 0.905±0.005 | 1.01±0.01 | 0.372±0.003 | 0.391±0.003 | 0.095±0.005 | 0.216±0.001 | <0.2 |
| SSSw2II | 0.37±0.01 | 1.314±0.003 | 0.401±0.005 | 0.32±0.01 | 0.115±0.005 | 0.123±0.001 | <0.2 |

Cooling mode: a = air cooling; w1 = immersion; w2 = quenching

< LOQ = below limit of quantification

n.a. = not analysed

|  | P | Mo | Ba | Sr | Na | K | Cu |
| --- | --- | --- | --- | --- | --- | --- | --- |
| c/mg kg–1 |  |  |  |  |  |  |  |
| Sa | 137±2 | 470±20 | 251±5 | 514±2 | 480±10 | 193±3 | 412±30 |
| Sw | 164±2 | 440±40 | 270±2 | 492±2 | 440±20 | 142±9 | 450±40 |
| SaT | n.a. | 450±50 | 180±20 | 495±1 | 480±30 | 111±2 | 400±20 |
| SwT | n.a. | 260±20 | 269±11 | 495±7 | 390±10 | 87±4 | 250±10 |
| E3041 | 137±2 | 250±30 | 259±1 | 474±5 | 1320±10 | 157±8 | 145±8 |
| E3042 | 120±7 | 320±10 | 248±1 | 438.0±0.1 | 1200±90 | 160±30 | 200±1 |
| E31 | 161±1 | 2100±200 | 560±10 | 485±6 | 1110±30 | 158±5 | 290±40 |
| E32 | 127±4 | 2100±100 | 548±1 | 482±3 | 1100±100 | 170±40 | 310±60 |
| EM1 | 648±7 | 158±7 | 309±1 | 627±2 | 1513±5 | 290±20 | 113±1 |
| EM2 | 630±20 | 290±60 | 314±6 | 501±1 | 1240±40 | 230±20 | 150±10 |
| CSa | 57±4 | 240±20 | 820±1 | 263±3 | 260±10 | <25 | 356±4 |
| CSw1 | 116±2 | 330±40 | 771±6 | 261±1 | 258±3 | <25 | 490±80 |
| CSw2 | 85±7 | 360±50 | 811±1 | 255±3 | 270±40 | <25 | 570±70 |
| SSa | 107±2 | 350±4 | 209±1 | 176±1 | 218±4 | <25 | 283±2 |
| SSw1 | 103±2 | 420±30 | 174±2 | 165±1 | 204±5 | <25 | 310±20 |
| SSw2 | 130±10 | 440±40 | 198±1 | 177±1 | 188±5 | <25 | 300±20 |
| SSSa | 120±10 | 410±20 | 222±1 | 380±1 | 392±11 | 103±5 | 279±5 |
| SSSw1I | 96±9 | 440±20 | 178±3 | 386±3 | 301±9 | 77±1 | 276±2 |
| SSSw1II | 91.6±0.1 | 280±30 | 245±3 | 393±3 | 276±4 | 81±1 | 210±20 |
| SSSw2I | 96±4 | 450±10 | 252±4 | 397±1 | 345±1 | 111±1 | 280±10 |
| SSSw2II | 87±4 | 2500±300 | 297±5 | 370±10 | 312±8 | 43±1 | 229±3 |

Cooling mode: a = air cooling; w1 = immersion; w2 = quenching

< LOQ = below limit of quantification

n.a. = not analysed

|  | Co | Zn | Pb | As | Cd | Se |
| --- | --- | --- | --- | --- | --- | --- |
| c/mg kg–1 |  |  |  |  |  |  |
| Sa | 114±8 | 226±5 | <5 | 4.2±0.2 | <1 | <5 |
| Sw | 120±30 | 87±4 | <5 | 7±1 | <1 | <5 |
| SaT | 110±4 | 90±1 | 5.1±0.2 | 7.9±0.1 | <1 | <5 |
| SwT | 67±1 | 83±1 | 5.9±0.1 | 3.6±0.1 | <1 | <5 |
| E3041 | 43±2 | 150±20 | <5 | 6±1 | <1 | <5 |
| E3042 | 60±1 | 58±4 | <5 | 6.6±0.3 | <1 | 6±1 |
| E31 | 140±7 | 30±2 | <5 | 8.3±0.4 | <1 | 7±1 |
| E32 | 150±8 | 38±6 | <5 | 9±1 | <1 | 6±1 |
| EM1 | 23±2 | 270±40 | <5 | 8.5±0.5 | <1 | <5 |
| EM2 | 35±1 | 246±5 | <5 | 9.8±0.2 | <1 | <5 |
| CSa | 128±1 | 15±2 | <5 | 4,2±0,2 | <1 | <5 |
| CSw1 | 160±30 | 23±1 | <5 | 7±1 | <1 | <5 |
| CSw2 | 210±20 | 19±1 | <5 | 6±1 | <1 | <5 |
| SSa | 94±1 | 19±1 | <5 | 6.6±0,3 | <1 | 6±1 |
| SSw1 | 106±7 | 20±1 | <5 | 8.3±0,4 | <1 | 7±1 |
| SSw2 | 98±8 | 40±1 | <5 | 9±1 | <1 | 6±1 |
| SSSa | 91±2 | 61±4 | <5 | 8.5±0,5 | <1 | <5 |
| SSSw1I | 90±1 | 57,8±0,1 | <5 | 9.8±0,2 | <1 | <5 |
| SSSw1II | 64±5 | 55±2 | <5 | 6.7±0,6 | <1 | <5 |
| SSSw2I | 85±3 | 82±1 | <5 | 8.8±0,4 | <1 | <5 |
| SSSw2II | 66±5 | 440±70 | <5 | 5.8±0,3 | <1 | <5 |

Cooling mode: a = air cooling; w1 = immersion; w2 = quenching

< LOQ = below limit of quantification

n.a. = not analysed

Table S2. Basicity of investigated slags expressed as B and Mb.

| # Sample | B = w(CaO)w (SiO2) | Mb = wCaO+w(MgO)wSiO2+w(Al2O3) |
| --- | --- | --- |
| Sa | 1.85 | 1.72 |
| Sw | 1.81 | 1.70 |
| SaT | 1.82 | 1.70 |
| SwT | 1.85 | 1.73 |
| E3041 | 2.20 | 1.89 |
| E3042 | 2.06 | 1.95 |
| E31 | 1.62 | 1.68 |
| E32 | 1.63 | 1.65 |
| EM1 | 4.04 | 2.06 |
| EM2 | 1.88 | 1.47 |
| CSa | 2.06 | 1.90 |
| CSw1 | 2.13 | 1.89 |
| CSw2 | 2.04 | 1.87 |
| SSa | 1.76 | 1.78 |
| SSw1 | 1.77 | 1.80 |
| SSw2 | 1.88 | 1.87 |
| SSSa | 1.97 | 1.81 |
| SSSw1I | 1.90 | 1.77 |
| SSSw1II | 1.85 | 1.75 |
| SSSw2I | 1.92 | 1.79 |
| SSSw2II | 1.63 | 1.62 |

Table S3. BET surface and average pore diameter of the investigated EAF S slags. The average pore diameter (4V/A) was calculated from the desorption part of the curve.

| Sample | fraction/ mm | m/ g | BET/ m2 g–1 | Average pore diameter /nm* |
| --- | --- | --- | --- | --- |
| CSa | 0–1 | 8.7434 | 0.0980 | 15.088 |
|  | 1–4 | 13.8383 | 0.0172 | 16.151 |
| CSw1 | 0–1 | 14.3889 | 0.2865 | 18.088 |
|  | 1–4 | 10.4928 | 0.1255 | 13.376 |
| CSw2 | 0–1 | 2.6127 | 0.1310 | 17.271 |
|  | 1–4 | 8.1260 | 0.0610 | 10.460 |
| SSa | 0–1 | 9.7337 | 0.3625 | 18.446 |
|  | 1–4 | 11.3925 | 0.0865 | 23.071 |
| SSw1 | 0–1 | 10.8135 | 0.4187 | 17.904 |
|  | 1–4 | 8.5893 | 0.1264 | 18.97 |
| SSw2 | 0–1 | 8.2863 | 0.4534 | 18.414 |
|  | 1–4 | 9.6351 | 0.1297 | 15.927 |

Cooling mode: a = air cooling; w1 = immersion; w2 = quenching

Figure S1. The presence of γ-Ca2SiO4 in the powdered samples.

Figure S2. Particle size distribution of samples CSa, CSw1 and CSw2 ,and of samples SSa, SSw1 and SSw2

Figure S3. Particle size distribution of samples SSSa, SSSw1I, SSSw1II, SSSw2I and SSSw2II.

Figure S4. Particle size distribution of samples E3041, E3042, E31, E32, EM1 and EM2.