Abbreviations:

MIH - hypomineralized enamel

HE - normal enamel (healthy teeth)

Table 1 ﻿The concentration profile of chemical elements of hypomineralized and healthy tooth enamel expressed in atomic percentage

| Parameter | C |  | P |  | Ca |  | O |  | Ca-P |  | Ca-C |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tooth * | MIH | HE | MIH | HE | MIH | HE | MIH | HE | MIH | HE | MIH | HE |
| number of data | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 |
| md | 18.27 | 17.30 | 10.01 | 10.64 | 16.63 | 17.39 | 54.27 | 54.10 | 1.66 | 1.64 | 0.92 | 1.01 |
| sd | 1.32 | 0.97 | 0.60 | 0.95 | 0.96 | 0.62 | 0.31 | 0.29 | 0.05 | 0.11 | 0.12 | 0.09 |
| Sig. хз | <0.000 |  | <0.000 |  | <0.000 |  | <0.000 |  | 0.007 |  | <0.000 |  |

Table 2 ﻿The concentration profile of chemical elements of hypomineralized and healthy tooth enamel expressed in weight percentage

| Parameter | C |  | P |  | Ca |  | O |  | Ca-P |  | Ca-C |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tooth * | MIH | HE | MIH | HE | MIH | HE | MIH | HE | MIH | HE | MIH | HE |
| number of data | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 |
| md | 11.70 | 10.94 | 14.52 | 15.05 | 27.60 | 28.80 | 44.72 | 43.77 | 1.90 | 1.91 | 2.39 | 2.65 |
| sd | 1.06 | 0.95 | 0.78 | 0.60 | 1.47 | 1.03 | 1.25 | 0.90 | 0.05 | 0.04 | 0.36 | 0.28 |
| Sig. хз | <0.000 |  | <0.000 |  | <0.000 |  | <0.000 |  | <0.000 |  | <0.000 |  |

Graph 1  ﻿The distribution of calcium concentration at the examined points of the tooth going from the tooth surface to the enamel-dentine border.

Graph 2  ﻿The distribution of phosphorus concentration at the examined points of the tooth going from the tooth surface to the enamel-dentine border.﻿

Graph 3  ﻿The distribution of carbon concentration at the examined points of the tooth going from the tooth surface to the enamel-dentine border.﻿

Graph 4 ﻿The ratio of calcium / phosphorus concentration at the examined points of the tooth going from the tooth surface to the enamel-dentine border

Graph 5 ﻿The ratio of calcium / phosphorus concentration at the examined points of the tooth going from the tooth surface to the enamel-dentine border